## Slide 1
1st Workshop on Advanced Neutron Source and its Application
Design and technical challenges of Li target for IFMIF-based neutron sources
Davide BERNARDI (ENEA)
4-5 November, 2017 Aomori-city, Japan

## Slide 2: Outline
IFMIF Li target concept
TA design basis
TA lifetime-related issues:
  Irradiation embrittlement
  Erosion/corrosion
  Loss of gaskets performance
  Other phenomena
Summary and conclusions

## Slide 3: IFMIF Li target concept
High Flux Test Module (HFTM)
d+7Li
n+2α
d+7Li
n+8Be
n+p+7Be
d+7Li
2n+7Be
n+p+t+α
d+7Li
d+7Li
d+6Li
d+6Li
d+6Li
d+6Li
n+7Be
n+α+3He
n+p+6Li
n+p+d+α

## Slide 4: TA design basis /1
maintain a stable high-velocity, free surface flow of liquid lithium in front of the D+ beam
produce the adequate neutron flux to properly irradiate the test modules
remove the high thermal power deposited in the lithium jet by the D+ beam
Parameter | Value
Beam power | 10 MW (IFMIF) 5 MW (DONES)
Beam current | 250 mA (IFMIF) 125 mA (DONES)
Beam energy | 40 MeV
Beam footprint area | 20x5 cm2 (nominal) 10x5 cm2 (optional in DONES)
Surface heat flux | 1 GW/m2 (IFMIF) 500 MW/m2 (DONES)
Li channel width | 260 mm
Li velocity | 15 m/s (nominal)
Li inlet temperature | 250 °C (nominal)
Li jet thickness | 25 mm ± 1 mm
Vacuum pressure | 10-3 Pa
BP channel minimum thickness | 1.8 mm
Beam angle | 9°
Nozzle vertical inclination | 22.5°
BP distance to HFTM | 2  1 mm
Materials | RAFM steel 316L
Availability | 94 %
Li channel

## Slide 5: TA design basis /2
Li channel profile developed by ENEA
Pressure distribution
Variable curvature profile allowing for gradual pressure increase to limit flow disturbances
Successfully tested in ELTL (Oarai, Japan) within IFMIF/EVEDA
Damage rate [dpa/fpy] (DONES)
Avoid Li boiling
Create smooth pressure distribution
Backplate thermal field (DONES)
Tmax = 300°C

## Slide 6: TA design basis /3
Bayonet BP concept
Average nuclear responses on the BP footprint volume
IFMIF conditions (two accelerators – 10 MW beam)
The BP is the TA most critical component due to severe irradiation and harsh working conditions
BP lifetime is expected to be limited and its assessment is crucial to performance and maintenance
Replacement of BP/TA is needed at some time:
  Bayonet concept: only the BP is replaced
  Integral concept: all the TA is replaced
M. Frisoni et al. “Nuclear analysis of the IFMIF European lithium target assembly system, Fusion Engineering and Design, 89 (2014), 1959-1963
Integral TA concept
Fast Disconnecting System (FDS)
No gasket needed
Simplified design
Maintenance not optimized
More waste generated
Low activated waste
Maintenance optimized
Sealing gasket needed
Complex design

## Slide 7: TA lifetime related issues
Main life-limiting factors for the Li target:
Irradiation embrittlement (Lemb)
Erosion/corrosion by high-speed Li flow (Lcorr)
Loss of sealing gaskets performance (Lgask)
Other phenomena (swelling, creep,…)
TA lifetime = min (Lemb, Lcorr, Lgask, ...)

## Slide 8: Irradiation embrittlement /1
Irradiation in Fast spectrum Reactors (HFR, BR2, BOR60) within different EU programmes (SPICE, ARBOR,…)
E. Gaganidze, J. Aktaa, Assessment of neutron irradiation effects on RAFM steels, Fusion Engineering and Design 88 (2013) 118–128
Radiation damage effect
Strong DBTT increase at low doses, saturation beyond 15 dpa, slow increase up to ~70 dpa
Large scatter of DBTT (unirrad.) but always lower than -50 °C
DBTT ~120°-125°C@30dpa (DONES), ~140°C-150°C@60 dpa (IFMIF)
He effect strongly enhances embrittlement in the concerned T range
Neutron irradiation of B-doped steel technique probably largely overestimates He embrittlement
Extra ∆DBTT = ∆DBTT(doped) - ∆DBTT(non-doped)
1 fpy irradiation in DONES
He effect
boron-doped EUROFER-like steels

## Slide 9: Irradiation embrittlement /2
Influence of temperature on DBTT shift
dpa-induced DBTT shift
DBTT shift much more sensitive at lower temperatures (< 350 °C)
Possible mitigating actions:
  increase TA operating temperature to ~350-360°C (limited by swelling)
  Thermal annealing at high temperature (550°C/3 h)
He-induced DBTT shift
B-doped
Non-doped
E. Gaganidze, J. Aktaa, Assessment of neutron irradiation effects on RAFM steels, Fusion Engineering and Design 88 (2013) 118– 128

## Slide 10: Erosion/corrosion
Material: EUROFER 97
Li speed = 15 m/s
T = 330 °C
N concentration ~30 wppm
duration: 4000 hours
Recent LIFUS-6 results:
Erosion/corrosion is seen to play no role on the BP lifetime
Max corrosion rates observed: ~0.25 µm/y in 4000 h
LIFUS-6 @ ENEA Brasimone
IFMIF/EVEDA validation results

## Slide 11: Loss of sealing gaskets performance
Helicoflex HNV 200 sealing gasket
Suitability of the gasket proved only up to 5500 h
Test @ 5500 h: no leakage
Test @ 7000 h: leakage observed
Post-test analysis after 7000 h exposure
Test results:
but…suspect of some uncontrolled conditions in the 7000 h test →
more long-term tests are needed
T=350 °C
N conc. in Li < 300 wppm (certified by supplier)
Exposure tests to stagnant Li were performed up to 7000 h at ENEA Brasimone within IFMIF/EVEDA validation activities
Test conditions:
Outer jacket : soft iron
Spring: Nimonic 90
Inner lining: AISI 304

## Slide 12: Other phenomena
Thermal creep
According to RCC-MRx (Tome 6), for temperatures below 375°C EUROFER thermal creep is negligible whatever the holding time, thus at the TA operating temperature this effect is not significant
Swelling
For temperatures below 360 °C the Japanese RAFM steel F82H irradiated with heavy ion beams shows a negligible swelling up to 50 dpa. EUROFER is also reported to show long swelling incubation times at low temperatures (Material Property Handbook, EUROfusion WPMAT) and therefore this effect is expected to be not relevant for the TA
Irradiation creep
EUROFER presents a very low irradiation-creep deformation (less than 1%) after irradiation for 63 dpa at 325°C (A. Alamo, Post-Irradiation Examinations (PIE) of materials irradiated in BOR60 at 325°C up to 42 dpa Final Report - TW2-TTMS-001-D02)

## Slide 13: Summary and conclusions
A rough assessment of the factors limiting the TA lifetime has been carried out based on available literature and experimental data
Two issues seem to be the most critical: irradiation embrittlement of F/M steel and loss of gasket performance
In the concerned temperature range, strong DBTT shift is expected even at low doses due to both displacement damage and He production effects
As a possible countermeasure, an increase of the TA operating temperature (up to ~350°-360 °C) or a thermal annealing could be considered to partially overcome or recover the irradiation embrittlement
Gasket integrity has been proved only until 5500 h
However…gasket exposure test @ 7000 h may have been jeopardized by some unexpected event (air entrance, oxidations,…) → a more extensive test campaign is needed for the full qualification of the gasket (possibly taking into account also irradiation)

## Slide 14
Thank you

## Slide 15: Irradiation embrittlement /3
∆DBTT [°C]
Dose [dpa]
Radiation damage effect
extra He effect
Total ∆DBTT(rad. damage + He)
Based on 13 appm He/dpa (evaluated from nuclear analysis of TA under DONES conditions)

## Slide 16: Irradiation embrittlement /4
DBTT [°C]
Dose [dpa]
BP operating temperature: ~250-300 °C
DBTT = -90 °C + ΔDBTT total
BP lifetime ~20 dpa → 20/30*12 ~ 8 months
DBTT of unirradiated EUROFER
BP thermal field under DONES conditions (5 MW beam)
Lifetime estimation due to dpa+He embrittlement
1 fpy irradiation
Rather conservative due to probable
overestimation of He-induced effect in B-doped steel

## Slide 17: Swelling
E. Wakai et al., Effect of gas atoms and displacement damage on mechanical properties and microstructures of F82H, Journal of Nuclear Materials 356 (2006) 95–104
Dual-beam ion irradiation was performed:
Fe3+ ions @ 10.5 MeV
He+ ions @ 1.05 MeV
50 dpa
10-15 appm He/dpa (controlled by energy degraders)
F82H @
50 dpa, 10-15 appm He/dpa
Swelling negligible below 360 °C
Max. volumetric swelling @ 430 °C (~0.6%)
Since BP operating T is < 360 °C swelling is not expected to be an issue
Literature data not available for EUROFER (only for F82H)

## Slide 18: Irradiation embrittlement /1
Irradiation-induced DBTT shift of EUROFER 97
KSLT and standard ISO CV specimens
irradiated @ T < 350 °C
CHARPY tests - criterion: 50% of USE
KSLT (mini-CV) specimens irradiated @ 250°- 340°C
CHARPY tests - criterion: 50 J/cm2
EUROfusion WPMAT, Material Property Handbook